## Slide 1: Particle Synthesis
Kamala Albrecht, YSP Student, Winchester High School
Nathan Hammerschmitt Le Gal, YSP Student, Essex North Shore Agricultural and Technical School
Sabrina Marnoto, Chemical Engineering, Northeastern University
Assistant Professor Sara M. Hashmi, Chemical Engineering, Northeastern University
Using Macro and Micro Fluidic Devices

## Slide 2: Goal
Synthesize microparticles with a tunable softness that can be used to study different complex fluid phenomenon.
Complex Fluid = Dispersed in Continuous (ex. Milk or sand)
  Model complex fluid phenomenon
  Blood flow, particle sorting
Key Characteristics
Large batches
  Ease of cost, time, etc.
Monodispersed
  Uniform in size and shape - ideally spherical
Stability over time
  Resuspendability
Once particles are created,
Mechanical testing
  How squishy (modulus)
  Size

## Slide 3: Big Picture
Fundamental Application: To better understand how particle softness affects particle flow.
Vascular Occlusions
Thrombosis (Detrimental blood clotting)
Pharmaceuticals (Drug delivery)

## Slide 4: Macro Devices
Syringe pump
  Controlled force on syringe for accuracy and precision
  Apparatus made using tubing and epoxy
  Droplet size controlled via syringe diameter

## Slide 5: Micro Devices
Microfluidic Device
  Micron sized channels
  Use microscope to view
Emulsion method
  Hydrophobic oil forms droplets
  Gel droplets once formed

## Slide 6: Sodium Alginate
Alginate in Syringe
Used syringe to form alginate droplets that crosslink in calcium
Alginate concentrations were varied
Calcium Chloride concentrations were varied
Particles were large (2mm)
Modulus correlate with its varied solution
Alginate in Microfluidic Droplet-Maker
Water in water system was difficult to tune
Viscosities needed additional adjustments
Moved on to vPDMS (oil in water system)

## Slide 7: Sodium Alginate Results

## Slide 8: vPDMS
vPDMS Emulsification
Because oil and water do not mix, the vPDMS forms droplets when combined
By agitating the droplets, they break into smaller and smaller pieces
  They are then gelled in a similar way to Alginate, using a crosslinker
Ratios of Crosslinker and Catalyst were varied (1:3, 1:1, 3:1)
Measured using Dynamic Light Scattering (DLS)
Particles were incredibly small (~200 nanometers)
  High range or polydispersity
Time agitated in Sonicator (uses sound wave vibrations) also varied
  15 min, 30 min, 1 hr
  Average size of particles correlated to time in Sonicator
Dynamic Light Scattering (DLS)
Sonicator

## Slide 9: vPDMS Results

## Slide 10: Conclusion and Future Steps
2 Direct Relationships
Sonication time and size
CaCl2% and Modulus
If we had more time…
Do more experimenting to control Polydispersity
  Filtering, Sieving, etc.
Adjust droplet maker parameters
  Setup and clean up makes droplet maker hard to work with

## Slide 11: References and Acknowledgements
https://www.cospheric.com/UV_fluorescent_microspheres_beads_powders.htm
https://www.healthspectra.com/how-to-improve-blood-circulation/
\https://www.yumpu.com/en/document/view/22180014/model-11-syringe-pump-series-manual-harvard-apparatus
https://www.precigenome.com/droplet-emulsion-based-microparticle-synthesis
Water-in-water droplets by passive microfluidic flow focusing. ACS Publications (2016). Available at: https://pubs.acs.org/doi/10.1021/acs.analchem.6b00225
https://www.gavi.org/vaccineswork/what-blood-clotting-disorder-astrazeneca-vaccine-has-been-linked
https://www.news-medical.net/health/Blood-Clotting-Process.aspx
https://www.knowledgeablefact.com/pharmaceutical-emulsions
Moon, B.-U., Hwang, D. K., & Tsai, S. S. H. (2016). Shrinking, growing, and bursting: microfluidic equilibrium control of water-in-water droplets. In Lab on a Chip (Vol. 16, Issue 14, pp. 2601–2608). Royal Society of Chemistry (RSC). https://doi.org/10.1039/c6lc00576d
Moon, B.-U., Abbasi, N., Jones, S. G., Hwang, D. K., & Tsai, S. S. H. (2016). Water-in-Water Droplets by Passive Microfluidic Flow Focusing. In Analytical Chemistry (Vol. 88, Issue 7, pp. 3982–3989). American Chemical Society (ACS). https://doi.org/10.1021/acs.analchem.6b00225
Rezvantalab, H., & Shojaei-Zadeh, S. (2013). Particle adsorption at polydimethylsiloxane (PDMS)/water interfaces in the presence of a cross-linking reaction. In Journal of Colloid and Interface Science (Vol. 400, pp. 70–77). Elsevier BV. https://doi.org/10.1016/j.jcis.2013.02.048
Taha, A., Ahmed, E., Ismaiel, A., Ashokkumar, M., Xu, X., Pan, S., & Hu, H. (2020). Ultrasonic emulsification: An overview on the preparation of different emulsifiers-stabilized emulsions. In Trends in Food Science &amp; Technology (Vol. 105, pp. 363–377). Elsevier BV. https://doi.org/10.1016/j.tifs.2020.09.024
Principal Investigator
Sara M. Hashmi
Lab Members
Sabrina Marnoto
Olukayode Majekodunmi
Saeed Alborzi
Kamala Albrecht (YSP)
Nathan Hammerschmitt Le Gal (YSP)
Center of STEM Education
Claire Duggan
Nicolas Fuchs
Franklin Ollivierre III
Katherine Aristizabal Norena